## Slide 1: How to Scale Buoyant Flake Formulation and Manufacture
Author: Sev Clarke Dec 2022

## Slide 2: Phasing
To restore global ocean health and productivity; to increase its cooling albedo enough to offset current levels of greenhouse gas warming; and to sequester substantial quantities of CO2 in its depths, supplementary nutrients of the eventual order of hundreds of megatonnes per annum of Buoyant Flakes would be required.
To go from making a few kilograms of flake in order to optimize its formulation, to an industry producing megatonnes of flake by, say, 2040 requires some four phases. The scales of these may conveniently be termed the Kilogram, Tonne, Kilotonne and Megatonne phases. The methods to be used for each of the first two phases are outlined below. Except for a few suggestions, those for the latter two phases require the services of professional engineering and logistics practitioners. Phases will overlap.

## Slide 3: Kilogram-scale flake manufacture
For laboratory and mesocosm testing of Buoyant Flake performance and effects only kilogram-scale quantities are required. Low cost and ease of sourcing and construction are more the issue than are wastage, formulation or process efficiency. Hence: the flakes are probably not pre-flattened; the waste minerals are simulated from local sources; the processing is of a handcrafted nature; and the baking process domestic.
The main equipment consists of long, thick garden stakes, clingwrap, corrugated PVC/PC sheet, trolleys, rope, rakes, step ladder, sieving pan, high-volume low-pressure (HVLP) paint spray gun(s), and a domestic microwave oven.
Flake materials might comprise: sacked rice husks sold as animal bedding; commercial Organosolv lignin powder; iron oxide cement colourant; garden supply powdered phosphate rock; home-made, rice water glue; and possibly a leavening agent such as baking powder (or possibly into recoverable ammonium bicarbonate which decomposes above 360C into NH3 and CO2 gases plus water) - unless there is enough water left in the partly-dried rice water glue and air between the powdered particles to leaven the flakes in baking whilst the lignin glue hot-melts then cools to form a strong, buoyant and waterproof matrix.

## Slide 4
Supporting trolleys
under the sheet
Kilogram-scale
Flake “Factory”
Step ladder
Hand-shaken sieve provides a
steady shower of rice husks or
semi-coated, buoyant flakes
Lignin-mineral-leavening mix to
be spread over the corrugated
PVC/PC plastic sheet
Mix and glue-moistened husks or flakes
are shaken together by being drawn
over transverse, corrugated plastic sheeting
so each husk is thoroughly coated in the mix.
After partial drying, more layers may be
added before the baking operation
generates hard, leavened Buoyant Flakes
Microwave oven
A spray paint gun
sprays a mist of rice
water glue, suffusing
the open chamber.
Larger droplets might
be left to impact the
opposite wall
Film plastic Clingwrap
covers wooden framework
that is open at both top
and bottom
After passing through the coating
operations, flakes are raked off
and fed into the oven, possibly
including balls of glued mix not
attached to husks
The sheet might be given low sides
in order to retain the mix better.
The mix should be thick enough
to cover the corrugations
Rope

## Slide 5: Tonne to low-kilotonne-scale Pilot Flake Factory
Such a factory might use rice husks that had been flattened and densified for transportation by passing them through heated rollers after being sprayed with rice water glue.
Materials for flake production at these scales might consist of: packaged rice husks (flattened or otherwise); packaged or bulk lignin powder; bulk powdered rock phosphate; bulk haematite or iron ore fines, and possibly much smaller amounts of the packaged oxides of several transition metals, plus cerium, selenium, strontium, etc. The relative amounts of these trace element flake constituents might resemble those calculated in a separate document and designed specifically for nutriating methanotrophs.
The version 11 buoyant flake mix of 2012 was suggested to be husk:lignin:Fe+P+trace minerals in the ratio by weight of 60:15:25. However, the more recent addition of rice water glue and a leavening agent would probably allow the husk content to be substantially reduced, perhaps to a finished flake ratio of husk:lignin:haematite:rock phosphate = 100:69:81:244 (or percentages of 20:14:16:49% with other minor residues). Experimentation will determine what are optimal proportions to be used, both on average and for each regional ocean environment and season. A prospective leavening agent is urea (NH2)2CO which may, in the presence of water, decompose at 160-1800C and higher into the gases NH3, CO2 and H2O. Alternatives include di-ammonium tartrate and potassium sodium tartrate tetrahydrate. The leavening agent might best be dissolved into the rice water glue before use. Raw flakes heated by infra-red lamps and/or microwaving might at first form a skin of melted lignin and minerals that contained the later-releasing gases to form a foam with a husk core that cools into a durable, buoyant, ammonia-rich, expanded flake product. Reducing the lignin content to near the minimum required for long term flake buoyancy would improve the economics.
The factory might not be in one of the eight, preferred global manufacturing sites, but would probably have to import most of its materials. Its products might well be used in several global locations for testing purposes, each possibly requiring a separate mineral formulation. Economically, the pilot factory might take over the facilities of an unused food processing or baking facility, as the processes are somewhat similar. Once the husks had been coated in an optimal number of layers or shells of misted rice water glue then mineral mix+lignin+leavening agent, and then partly dried, baking of the separated flakes on a conveyor belt might prove best, as it would tend to melt the Organosolv lignin hot-melt glue (m.p.154-1620C) throughout each flake before too much volatile material had left it, thereby probably ensuring both leavened buoyancy and a suitably strong, water-resistant bonding. Flakes might resemble lightweight, thickened, red rice grains that would turn green in the ocean when colonized by phytoplankton.
The factory would probably still use fossil fuels for drying and heating, rather than solar heat or other renewable energy source; and it would not necessarily have port facilities and infrastructure for a major, bulk shipping operation.
The factory’s purchasing and logistics operations would probably not be under long term contracts, and its staff might mainly be under short-term contracts, or else be seconded from organizations intending to become leaders in the new industries.
As the scale of operations increases, consideration should be given to the optimal changeover points to the use of the much cheaper and more sustainable, if less nutrient-rich, minerals of red mud tailings, phosphatic clay wastes, and low-grade mineral resources. Also, to the use of concentrated solar heat for the drying and baking processes, the eight global flake manufacturing sites, and to customized vessels.

## Slide 6
Tonne to low Kilotonne-scale
Flake Factory Process
J
Rice water glue
misting chamber
Flattened rice
husk hopper
Semi-coated flake hopper
Shaken sieve determines
the flow rate and
even dispersion
Husk shower
Flake shower
Conveyor belt
Mix hopper
Recycled mix
Partly coated, drying flakes
Fully coated, drying flakes
Baked
flakes
Microwave
oven or tunnel
Vibrating sieve
separator
Vibrating conveyor belt
Vibrating conveyor belt
Air-heated belt
Bank of infra-red or warm,
dry air current heaters
Recycled material may require comminution
Misting nozzles